9.AWLGRIP PAINTSYSTEM FOR OLD & NEW POLYESTER BOATS - SURFACE BELOW THE WATERLINE


(MAXIMUM BARRIER SYSTEM)





Steps�
Product name�
Mixing ratio in volume plus reducer�
Recoat time in hours/weeks at 20°C�
Application method�
Abrasive paper    


grit�
Coverage per liter mix.�
Total wet film thickness�
Total dry film thickness�
Remarks�
�
9.1.�
Surface preparation: Surface Cleaner T340/


AwlPrep T0008�
N /A�
N / A�
N / A�
100-150�
N / A�
N / A�
N / A�
Make sure no contamination remains present on the surface !�
�
9.2.�
545 Anti-Corrosive Epoxy Primer  


�
Base	: 1     Grey D1001


Conv.	: 1             D3001


T0006	:  up to 25%�
In between coats :


min. :  2 hrs


max.: 24 hrs�
   Spray


�
80 - 120�
5 m² at 


60 micron�
175-250


micron


�
50-75 


micron�
May require multiple applications. It’s recommended to apply the first coat by roller.�
�
�9.3. �
Awlfair 


Light Weight


Fairing Compound�
Base	: 1              D8020


Conv.	: 1              D7007


�
min. : 24 hrs


max.: N/A�
Knife





 Board�
40 - 80�
1m²/1mm�
N / A�
N / A �
Do not add thinner or reducer. Always sand in between coats !�
�
�9.4.�
Hull-Gard ER Epoxy Primer�
Kit - base + converter 73057


T0006 : up to 10%�
In between coats :


min.: 3 hrs


max.: 8 wks �
Spray





          Roller�
N / A �
5,6 m² at 


75 micron�
150 micron�
75 micron�
Roller application requires at least 2 coats.�
�
�9.5.�
Hull-Gard WB Epoxy Primer�
Kit - base + converter


Black 73152


White 73128


T0006 : up to 20%�
in between coats :


min. : 5 hrs


max.: 24 hrs�
Spray





             


          Roller�
 N / A�
3,2 m² at 200 micron�
400 micron�
300 micron�
Has to be applied in multiple coats.�
�
�9.6.�
AwlStar Gold Label Anti-Fouling�
BP 201 Charcoal Black


BP 401 Medium Green


BP 501 Light Blue


BP 502 Deep Blue


BP 701 Red


BP 802 White Lightning�
in between coats :


min.  : 4 hrs


max. : N/A�
Spray














          Roller�
N / A�
1,6 m² at 300 micron�
500-600 micron�
250-300 micron�
Has to be applied in multiple coats.


Allow drying time of 5 hours at 21°C between coats.


Allow overnight drying before launch.�
�



For further information regarding surface treatment, application methods and product information see the description Awlgrip paintsystem n°9 for old and new polyester boats - surface below the waterline + Awlgrip technical product datasheets.





Note: In case no fairing is required, after step 9.2.( application of 545 Epoxy Primer), one can proceed with step 9.4. (application of Hull-Gard ER Epoxy Primer). In this case in between the application of the 545 Primer and the Hull-Gard ER Primer an overcoating time of min. 8 hours and max. 24 hours at 20°C. must be respected! If the overcoating time of 24 hours is exceeded, the 545 Primer needs to be sanded with grit 150 prior to the application of the Hull-Gard ER.


U.S. PAINT - 09.10.1998











