Skipper’s Line Varnishes

POLIGLASS – Two component, fast drying polyurethane varnish  		Mixing Ratio: A+B 2 parts A + 1 part B

Clear varnish applied as a multicoat system in a short period of time 		Brush/Roller: 10-15% thinner 205

“6 coats a day” can be used as base coat when thinned by 50-100 %		Dust Dry: 15-20 minutes

can be polished with abrasive polishing products, can be over coated 		T Coverage: 10 m2 per litre for 50dry microns

with all Skipper’s Line Varnishes e.g.: Starwind UV, Skipper UV, 		Pot Life: A+B 4 hours at (20°C)

Acriglass UV etc..								Spray: 20-30% thinner 203

ACRIGLASS UV – Two Component high gloss polyacrylic varnish		Mixing Ratio: A+B  2parts A + 1 part B

Clear polyacrylic varnish, providing excellent flowing properties and 		Brush/Roller: 10-15% thinner 205 Spray: 20-30% 203	a 	durable flexible film, it has excellent sticking power to Teak and 		Dust Dry: 40-50 minutes

provides a great finish for Mahogany, long lasting resistance in the		T Coverage: 10-12 m2 per litre for 40dry microns			severe marine environment. Can be buffed or polished.			Pot Life: A+B 4-6 hours at (20°C)

SPACE CLEAR UV – Two Component high flowing gloss brushable 		Mixing Ratio: A+B 2parts A + 1 part B 		  	v	Varnish with outstanding flowing characteristics for both spray 			Brush Roller: 10-15% thinner 201 Spray: 10-20% 201		and brush finish. Formulated with UV filters for long term resistance. This 	Dust Dry: 30-60 minutes

part of the SPACE TO LINE and comes with a range of additives for 		T Coverage: 12 m² per litre

severe application conditions. 						Pot Life: A+B 2-4 hours at (20°C)

TOPKAPI UV – One component polyurethane gloss varnish 			Brush/Roller: 15-20% thinner 107 or 109 for over 20°C

Clear gloss polyurethane, non-yellowing for a long lasting finish in the		Touch Dry: 6 hours

marine environment, with addition of UV filters to withstand sun 		T Coverage: 12-14 m2 per litre at 40 dry microns

exposure								Spray: 10-20% thinner 900

STARWIND UV – One component traditional extra quality gloss varnish 		Brush/Roller: 10-15% thinner 107 or 109 for over 20°C

Gloss varnish with tung oil and phenolic resin with UV filters for extra 		Touch Dry: 8 hours

brilliant long lasting finish, provides high filling power and a very flexible 		T Coverage: 12-13 m2 per litre for 40 dry microns

film for a quality finish on exterior and interior.				Spray: 10-20% thinner 900

## Skipper’s Line range includes other exterior varnishes and one & two pack interior varnishes SUPERWIND, BEKOL LUCIDA , TOPKAPI OPACA, BEKOL OPACA, POLISATIN, POLIMAT and  VERILUX

# Easy To Use Application Guide For

BARE WOOD:				“6 COATS A DAY SYSTEM”

1st Coat	Poliglass should be thinned with thinner 203 by 50-100% depending on wood absorption, allowing the varnish to penetrate into the wood. Allowing 15-20 minutes between coats.

2nd Coat 	Without rubbing down after the application of the 1st coat, apply 2nd coat of Poliglass again thinned with thinner 203 by 50-100% to cover the grain.

3rd Coat 	Again without rubbing down, if the wood requires another thinned coat for wood absorption apply another thinned coat by 50-100%, if this is not required apply a coat of Poliglass thinned by only

10-15% with the flowing thinner 205.

4th, 5th , 6th Coat 	Without rubbing down in between, all additional coat to be applied thinned with thinner 205 by

10-15% to gain desired build up of the varnish. (Further coats can be applied as desired)

7th Coat 	After allowing the varnish to harden off over night or between 12-24 hours, flat back the varnish using a fine sandpaper to eliminate any runs or sags in the varnish in order to obtain a perfectly smooth surface to apply your desired top coat of Acriglass UV, Space Clear UV, Topkapi UV Starwind UV. (Rubbing down in between topcoats is recommend)

8th Coat 	A second coat of the topcoat is recommended of Acriglass UV, Space Clear UV,  Topkapi UV

or Starwind UV. (Further coats can be applied if required)

Note: The information is given to the best of our knowledge but since the conditions of use of our products are beyond our control, no warranty is given or to be implied in respect of such information.  We are, at all times, willing to study customer's specific requirements involving our products in order to enable their most effective use.  Dilution rates and drying times are to be considered only indicative, based on a temperature of 20°C (68°F), and may be subject to changes according to prevailing temperature, in presence of particular weather conditions or due to application procedures that may be effective at time of application. See also the indicative coating systems information for Wood, Steel, Aluminium and Fibreglass boats available on request. Before starting the application please read carefully all the safety precautions stated on the label of each can. A Safety Data Sheet for each product is  available on request. For further information please contact our Technical Department: Telephone 01634 815522  Fax 01634 815533 – skipperukltd@aol.com or visit our website www.aemmecolori.it/skippers