10. AWLGRIP PAINTSYSTEM FOR OLD & NEW POLYESTER BOATS - SURFACE BELOW THE WATERLINE


(ECONOMY SYSTEM)





Steps�
Product name�
Mixing ratio in volume plus reducer�
Recoat time in hours/weeks at 20°C�
Application method�
Abrasive paper    


grit�
Coverage per liter mix.�
Total wet film thickness�
Total dry film thickness�
Remarks�
�
10.1.�
Surface preparation: Surface Cleaner T340/


AwlPrep T0008�
N /A�
N / A�
N / A�
100-150�
N / A�
N / A�
N / A�
Make sure no contamination remains present on the surface !�
�
�10.2.�
Hull-Gard ER Epoxy Primer�
Kit - base + converter 73057


T0006 : up to 10%�
In between coats :


min. : 3 hrs


max.: N/A�
Spray





          Roller�
N / A �
1,4 m² at 


300 micron�
600 micron





�
300 micron





�
Has to be applied in multiple coats. It’s recommended to apply the first coat by roller�
�
�10.3.�
AwlStar Gold Label Anti-Fouling�
BP 201 Charcoal Black


BP 401 Medium Green


BP 501 Light Blue


BP 502 Deep Blue


BP 701 Red


BP 802 White Lightning�
in between coats :


min.  : 4 hrs


max. : N/A�
Spray














          Roller�
N / A�
1,6 m² at 300 micron�
500-600 micron�
250-300 micron�
Has to be applied in multiple coats.


Allow drying time of 5 hours at 21°C between coats.


Allow overnight drying before launch.�
�



For further information regarding surface treatment, application methods and product information see the description Awlgrip paintsystem n°10 for old and new polyester boats - surface below the waterline + Awlgrip technical product datasheets.





U.S. PAINT - 09.10.1998











