11. AWLGRIP PAINTSYSTEM FOR BARE / NEW WOOD - SURFACE ABOVE THE WATERLINE 





Steps�
Product name�
Mixing ratio in volume plus reducer�
Recoat time in hours/weeks at 20°C�
Application method�
Abrasive paper    


grit�
Coverage per liter mix.�
Total wet film thickness�
Total dry film thickness�
Remarks�
�
11.1.�
Surface preparation: Surface Cleaner T340 / AwlPrep T0008�
N /A�
N / A�
N / A�
80-120�
N / A�
N / A�
N / A�
For the sealcoat no filmthickness can be specified.�
�
11.2.�
545 Anti-Corrosive Epoxy Primer  


�
Base	: 1   White D8001


Conv.	: 1             D3001


T0006	: 40%  (spray)


T0031:  40%  (brush)�
�min. : 8 hrs


max.: 24 hrs�
Spray





          roller/


           brush   �
180-220


.�
N / A�
N / A


�
N / A�
Only needs to be sanded if overcoating time of 24 hours at 20°C. has been elapsed.�
�
11.3.�
545 Anti-Corrosive Epoxy Primer�
Base   : 1     White D8001


           : 1     Grey  D1001


Conv.  : 1               D3001


T0006 : up to 25%�
min.: 2 hrs


max.: 24 hrs�
Spray


�
80 - 120�
5 m² at 60 micron�
175-250 micron�
50-75 micron�
May require multiple applications. Filmthick-ness calculated for mixed base and converter reduced 25%.�
�
�11.4. �
Awlfair 


Light Weight


Fairing Compound�
Base	: 1              D8020


Conv.	: 1              D7007


�
min. : 24 hrs


max.: N/A�
Knife





 Board�
40 - 80�
1m²/1mm�
N / A�
N / A �
Do not add thinner or reducer. Always sand in between coats !�
�
11.5.�
Ultra - Build


Epoxy Primer �
Base	: 1	 D8008


Conv. 	: 1	 D3018


T0073	: 5-10 %�
In between coats :


min. : 2 hrs


max.: 12 hrs�
Spray�
120�
1.5 m²�
625-750 micron�
375-500


micron�
May require multiple applications.�
�
11.6.


�
545 Epoxy Primer �
Base 	: 1   White  D8001


    or	  1   Gray   D1001


Conv.	: 1              D3001


T0006	:  up to 25%�
In between coats :


min.:  2 hrs


max.: 24 hrs


 �
Spray�
220-400�
5 m²�
175-250 micron�
50-75


micron�
In case more coats are required, allow a curing time of min. 8 hours in between the various coats.�
�
11.7.


�
Awlgrip Polyester


Urethane Topcoat�
Base	: 1    see colorcard


Conv.	: 1              G3010


T0001/T0003 : max. 25%�
In between coats :


30-45 min.�
Spray�
220-400�
6 m²�
150-200 micron�
50-75 


micron�
See guidelines for topcoat application.�
�
OR�
Awlgrip Polyester


Urethane Topcoat�
Base	: 2    see colorcard


Conv. 	: 1              H3002


T0031	: max. 25 %�
In between coats : overnight�
Brush �
220-400 or Scotch-Brite�
9 m²�
100-150 micron�
50-75 


micron�
Has to be applied in multiple coats�
�



For further information regarding surface treatment, application methods and product information see the description Awlgrip paintsystem n°11 for bare / new wood - surface above the waterline + Awlgrip technical product datasheets.





U.S. PAINT - 09.10.1998











