12. AWLGRIP PAINTSYSTEM FOR BARE / NEW WOOD - SURFACE BELOW THE WATERLINE 


(MAXIMUM BARRIER SYSTEM)





Steps�
Product name�
Mixing ratio in volume plus reducer�
Recoat time in hours/weeks at 20°C�
Application method�
Abrasive paper    


grit�
Coverage per liter mix.�
Total wet film thickness�
Total dry film thickness�
Remarks�
�
12.1.�
Surface preparation: Surface Cleaner T340 / AwlPrep T0008�
N /A�
N / A�
N / A�
80-120�
N / A�
N / A�
N / A�
For the sealcoat no filmthickness can be specified.�
�
12.2.�
545 Anti-Corrosive Epoxy Primer  


�
Base	: 1   White D8001


Conv.	: 1             D3001


T0006	: 40%  (spray)


T0031:  40%  (brush)�
�min. :  8 hrs


max.: 24 hrs�
Spray





          roller/


           brush   �
180-220


.�
N / A�
N / A


�
N / A�
Only needs to be sanded if overcoating time of 24 hours at 20°C has been elapsed.�
�
12.3.�
545 Anti-Corrosive Epoxy Primer�
Base   : 1     White D8001


           : 1     Grey  D1001


Conv.  : 1               D3001


T0006 : up to 25%�
min.: 2 hrs


max.: 24 hrs�
Spray


�
80 - 120�
± 5 m²�
175-250 micron�
50-75 micron�
May require multiple applications. Filmthickness calculated for mixed base and converter reduced 25%.�
�
�12.4. �
Awlfair 


Light Weight


Fairing Compound�
Base	: 1              D8020


Conv.	: 1              D7007


�
min. : 24 hrs


max.: N/A�
Knife





 Board�
40 - 80�
1m²/1mm�
N / A�
N / A �
Do not add thinner or reducer. Always sand in between coats !�
�
�12.5.�
Hull-Gard ER Epoxy Primer�
Kit - base + converter 73057


T0006 : up to 10%�
In between coats :


min. : 3 hrs


max.: 8 wks�
Spray





          Roller�
N / A �
± 5,6 m²�
150 micron�
75 micron�
Roller application requires at least 2 coats.�
�
�12.6.�
Hull-Gard WB Epoxy Primer�
Kit - base + converter


Black 73152


White 73128


T0006 : up to 20%�
in between coats :


min. : 5 hrs


max.: 24 hrs�
Spray





             


          Roller�
 N / A�
± 2,0 m²�
400 micron�
300 micron�
Has to be applied in multiple coats.�
�
�12.7.�
AwlStar Gold Label Anti-Fouling�
BP 201 Charcoal Black


BP 401 Medium Green


BP 501 Light Blue


BP 502 Deep Blue


BP 701 Red


BP 802 White Lightning�
in between coats :


min. : 4 hrs


max.: N/A�
Spray














          Roller�
N / A�
± 1,6 m²�
500-600 micron�
250-300 micron�
Has to be applied in multiple coats.


Allow drying time of 5 hours at 21°C between coats.


Allow overnight drying before launch.�
�






For further information regarding surface treatment, application methods and product information see the description Awlgrip paintsystem n°12 for bare / new wood 


- surface below the waterline + Awlgrip technical product datasheets.














Note : In case no fairing is required, after step 12.3.( application of 545 Epoxy Primer), one can proceed with step 12.5. (application of Hull-Gard ER Epoxy Primer). 


In between 545 Primer and Hull-Gard ER allow overcoating time of 12 hours minimum and 24 hours maximum at 20°C.


If the overcoating time of 24 hours is exceeded the 545 Primer needs to be sanded with grit 100-150 prior to the application of the Hull-Gard ER.








							    U.S. PAINT - 09.10.1998











