13. AWLGRIP PAINTSYSTEM FOR BARE / NEW WOOD - SURFACE BELOW THE WATERLINE 


(ECONOMY SYSTEM)





Steps�
Product name�
Mixing ratio in volume plus reducer�
Recoat time in hours/weeks at 20°C�
Application method�
Abrasive paper    


grit�
Coverage per liter mix.�
Total wet film thickness�
Total dry film thickness�
Remarks�
�
13.1.�
Surface preparation: Surface Cleaner T340 / AwlPrep T0008�
N /A�
N / A�
N / A�
80-120�
N / A�
N / A�
N / A�
For the sealcoat no filmthickness can be specified.�
�
13.2.�
545 Anti-Corrosive Epoxy Primer  


�
Base	: 1   White D8001


Conv.	: 1             D3001


T0006	: 40%  (spray)


T0031:  40%  (brush)�
�min. :  8 hrs


max.: 24 hrs�
Spray





          roller/


           brush   �
180-220


.�
N / A�
N / A


�
N / A�
Only needs to be sanded if overcoating time of 24 hours at 20°C. has been elapsed.�
�
�13.3.�
Hull-Gard ER Epoxy Primer�
Kit - base + converter 73057


T0006 : up to 10%�
In between coats :


min. : 3 hrs


max.: N/A�
Spray





          Roller�
N / A �
± 1,4 m²�
600 micron�
300 micron�
Has to be applied in multiple coats. Allow overcoating time of min.3 hours at 20°C. in between coats !�
�
�13.4.�
AwlStar Gold Label Anti-Fouling�
BP 201 Charcoal Black


BP 401 Medium Green


BP 501 Light Blue


BP 502 Deep Blue


BP 701 Red


BP 802 White Lightning�
in between coats :


min.  : 4 hrs


max. : N/A�
Spray














          Roller�
N / A�
± 1,6 m²�
500-600 micron�
250-300 micron�
Has to be applied in multiple coats.


Allow drying time of 5 hours at 21°C between coats.


Allow overnight drying before launch.�
�






For further information regarding surface treatment, application methods and product information see the description Awlgrip paintsystem n°13 for bare / new wood 


- surface below the waterline + Awlgrip technical product datasheets.





							   U.S. PAINT - 09.10.1998











