14. AWLGRIP PAINTSYSTEM FOR COMPOSITE PEEL-PLY SUBSTRATES ABOVE THE WATERLINE





Steps�
Product name�
Mixing ratio in volume plus reducer�
Recoat time in hours/weeks at 20°C�
Application method�
Abrasive paper    


grit�
Coverage per liter mix.�
 Total wet film thickness�
Total dry film thickness�
Remarks�
�
14.1.�
Surface preparation: 


(see description Awlgrip system for Peel-Ply substrates)�
N / A�
N / A�
N / A�
N / A�
N / A�
N / A�
N / A�
An adhesion test with Hull-Gard ER Epoxy Primer is highly recommended !�
�
�14.2.�
Hull-Gard ER Epoxy  Primer Cream


�
Kit - base + converter 73057


T0006	:  up to 10%�
In between coats :


min. : 3 hrs


max.: 8 wks�
Spray





         Roller�
N / A�
± 5,6 m²�
150 micron�
75 


micron�
Roller application requires at least 2 coats.�
�
�14.3. �
Awlfair 


Light Weight


Fairing Compound�
Base	: 1              D8020


Conv.	: 1              D7007


�
min.:  24 hrs


max.: N/A�
Knife





 Board�
40 - 80�
1m²/1mm�
N / A�
N / A �
Do not add thinner or reducer. Always sand in between coats !�
�
14.4.�
Ultra - Build


Epoxy Primer �
Base	: 1	 D8008


Conv. 	: 1	 D3018


T0073	: 5-10 %�
In between coats :


min.: 2 hrs


max.: 12 hrs�
Spray�
120�
± 1,5 m²�
625-750 micron�
375-500


micron�
May require multiple applications.�
�
14.5.


�
545 Epoxy Primer �
Base 	: 1   White  D8001


    or	  1   Gray   D1001


Conv.	: 1              D3001


T0006	:  up to 25%�
In between coats :


min. : 2 hrs


max.: 24 hrs�
Spray�
220-400�
± 5 m²�
175-250 micron�
50-75


micron�
In case more coats are required, allow a curing time of min. 8 hours in between the various coats.�
�
14.6.


�
Awlgrip Polyester


Urethane Topcoat�
Base	: 1    see colorcard


Conv.	: 1              G3010


T0001/T0003 : max. 25%�
In between coats :


30-45 min.�
Spray�
220-400�
± 6 m²�
150-200 micron�
50-75 


micron�
See guidelines topcoat application.�
�
OR�
Awlgrip Polyester


Urethane Topcoat�
Base	: 2    see colorcard


Conv. 	: 1              H3002


T0031	: max. 25 %�
In between coats : overnight�
Brush �
220-400 or Scotch-Brite�
± 9 m²�
100-150 micron�
50-75 


micron�
Has to be applied in multiple coats.�
�



For further information regarding surface treatment, application methods and product information see the description Awlgrip paintsystem n°14 for composite peel-ply substrates above the waterline + Awlgrip technical product datasheets.


						            U.S. PAINT - 09.10.1998


 











