2. AWLGRIP PAINTSYSTEM FOR STEEL BELOW THE WATERLINE 





Steps�
Product name�
Mixing ratio in volume plus reducer�
Recoat time in hours/weeks at 20°C�
Application method�
Abrasive paper    


grit�
Coverage per liter mix.�
Total wet film thickness�
Total dry film thickness�
Remarks�
�
2.1.�
Surface preparation: 


Sandblast�
N / A�
N / A�
N / A�
N / A�
N / A�
N / A�
N / A�
Surface profile 50 – 60 micron according to SIS Sa 2½�
�
�2.2.�
Hull-Gard ER Epoxy  Primer Cream


�
Kit - base + converter 73057


T0006	:  up to 10%�
In between coats :


min. : 3 hrs


max.: 8 wks�
Spray





          Roller�
N / A�
± 5,6 m² �
150 micron�
75 


micron�
Roller application requires at least 2 coats.�
�
�2.3. �
Awlfair 


Light Weight


Fairing Compound�
Base	: 1              D8020


Conv.	: 1              D7007


�
min.: 24 hrs


max.: N/A�
Knife





 Board�
40 - 80�
1m²/1mm�
N / A�
N / A �
Do not add thinner or reducer. Always sand in between coats !�
�
�2.4.�
Hull-Gard ER Epoxy Primer�
Kit - base + converter 73057


T0006 : up to 10%�
In between coats :


min. : 3 hrs


max.: N/A�
Spray





          Roller�
N / A �
± 5,6 m² �
150 micron�
75 micron�
Roller application requires at least 2 coats.�
�
�2.5.�
Hull-Gard WB Epoxy Primer�
Kit - base + converter


Black 73152


White 73128


T0006 : up to 20%�
in between coats :


min. : 5 hrs


max.: 24 hrs�
Spray





             


          Roller�
 N / A�
± 2,0 m²�
400 micron�
300 micron�
Has to be applied in multiple coats.�
�
�2.6.�
AwlStar Gold Label Anti-Fouling�
BP 201 Charcoal Black


BP 401 Medium Green


BP 501 Light Blue


BP 502 Deep Blue


BP 701 Red


BP 802 White Lightning�
in between coats :


min.  : 4 hrs


max. : N/A�
Spray














          Roller�
N / A�
± 1,6 m²�
500-600 micron�
250-300 micron�
Has to be applied in multiple coats.


Allow drying time of 5 hours at 21°C between coats.


Allow overnight drying before launch.�
�



For further information regarding surface treatment, application methods and product information see the description Awlgrip paintsystem n°2 for steel below the waterline  + Awlgrip technical product datasheets.





Note: In case no fairing is required, after step 2.2.(application of Hull-Gard ER), one can proceed with step 2.5.(application of Hull-Gard WB).














							   U.S. PAINT - 09.10.1998











