3. AWLGRIP PAINTSYSTEM FOR ALUMINUM ABOVE THE WATERLINE (WITH 545 PRIMER) 





Steps�
Product name�
Mixing ratio in volume plus reducer�
Recoat time in hours/weeks at 20°C�
Application method�
Abrasive paper    


grit�
Coverage per liter mix.�
Total wet film thickness�
Total dry film thickness�
Remarks�
�
3.1.�
Surface preparation: 


Deoxidine�
N / A�
N / A�
N / A�
36�
N / A�
N / A�
N / A�
Don’t let Deoxidine dry on the surface. Rinse thoroughly with water !�
�
3.2.�
545 Anti-Corrosive Epoxy Primer �
Base   : 1      Grey D1001


Conv. : 1               D3001


T0006:  up to 25%�
In between coats:


min. : 2 hrs


max.: 24 hrs�
Spray�
80 - 120�
± 4,0 m²�
250 micron�
75 micron�
May require multiple applications. Filmthick-ness calculated for mixed base and converter reduced 25%.�
�
�3.3. �
Awlfair 


Light Weight


Fairing Compound�
Base	: 1              D8020


Conv.	: 1              D7007


�
min.: 24 hrs


max.: N/A�
Knife





 Board�
40 - 80�
1m²/1mm�
N / A�
N / A �
Do not add thinner or reducer. Always sand in between coats !�
�
3.4.�
Ultra Build


Epoxy Primer�
Base	: 1              D8008


Conv.	: 1              D3018


T0073 : 5-10 %�
In between coats :


min. : 2 hrs


max.: 12 hrs�
Spray�
120�
± 1,5 m²�
625-750 micron�
375-500 micron�
May require multiple applications.�
�
3.5.�
545 Epoxy Primer�
Base	: 1  White   	D8001


or          1  Gray    	D1001


Conv.	: 1            	D3001


T0006	: up to 25 %�
In between coats :


min. : 2 hrs


max.: 24 hrs�
Spray





             


         �
 220-400�
± 5 m²�
175-250 micron�
50-75 micron�
In case more coats are required, allow a curing time of min. 8 hours in between the various coats.�
�
3.6.�
Awlgrip Polyester Urethane Topcoat �
Base	: 1  see colorcard 


Conv.	: 1            	G3010


T0001/T0003 : max. 25 %�
In between coats :


30-45 min.�
Spray�
220-400�
± 6 m²�
150-200 micron�
50-75 micron�
See guidelines for topcoat application.�
�
OR�
Awlgrip Polyester Urethane Topcoat�
Base	: 2  see colorcard 


Conv.	: 1            	H3002


T0031	: max. 25 %�
In between coats : overnight�
Brush�
220-400 or Scotch Brite�
± 9 m²�
100-150 micron�
50-75 micron�
Has to be applied in multiple coats.�
�



For further information regarding surface treatment, application methods and product information see the description Awlgrip paintsystem n°3 for aluminum above the waterline  + Awlgrip technical product datasheets.


U.S. PAINT - 09.10.1998











