4. AWLGRIP PAINTSYSTEM FOR ALUMINUM BELOW THE WATERLINE (WITH 545 PRIMER) 





Steps�
Product name�
Mixing ratio in volume plus reducer�
Recoat time in hours/weeks at 20°C�
Application method�
Abrasive paper    


grit�
Coverage per liter mix.�
Total wet film thickness�
Total dry film thickness�
Remarks�
�
4.1.�
Surface preparation: 


Deoxidine�
N / A�
N / A�
N / A�
36�
N / A�
N / A�
N / A�
Don’t let Deoxidine dry on the surface. Rinse thoroughly with water !�
�
4.2.�
545 Anti-Corrosive Epoxy Primer �
Base   : 1      Grey D1001


Conv. : 1               D3001


T0006:  up to 25%�
In between coats:


min. : 2 hrs


max.: 24 hrs�
Spray�
80 - 120�
5m² at 60 micron�
250 micron�
75 micron�
May require multiple applications. Filmthick-ness calculated for mixed base and converter reduced 25%.�
�
�4.3. �
Awlfair 


Light Weight


Fairing Compound�
Base	: 1              D8020


Conv.	: 1              D7007


�
min.: 24 hrs


max.: N/A�
Knife





 Board�
40 - 80�
1m²/1mm�
N / A�
N / A �
Do not add thinner or reducer. Always sand in between coats !�
�
�4.4.�
Hull-Gard ER Epoxy Primer�
Kit - base + converter 73057


T0006 : up to 10%�
In between coats :


min. : 3 hrs


max.: 8 wks�
Spray





          Roller�
N / A �
5,6 m² at 


75 micron�
150 micron�
75 micron�
Roller application requires at least 2 coats.�
�
�4.5.�
Hull-Gard WB Epoxy Primer�
Kit - base + converter


Black 73152


White 73128


T0006 : up to 20%�
in between coats :


min. : 5 hrs


max.: 24 hrs�
Spray





             


          Roller�
 N / A�
3,2 m² at 200 micron�
400 micron�
300 micron�
Has to be applied in multiple coats.�
�
4.6.�
Anti-Fouling suitable for aluminum�
N / A�
N \ A�
N / A�
N / A�
N / A�
N / A�
N / A�
Follow instructions manufacturer.�
�



For further information regarding surface treatment, application methods and product information see the description Awlgrip paintsystem n°4 for aluminum below the waterline  + Awlgrip technical product datasheets.





Note: In case no fairing is required, after step 4.2. (application of 545 Primer), one can proceed with step 4.4. (application of Hull-Gard ER). In between 545 Primer and Hull-Gard ER allow an overcoating time of 12 hours minimum and 24 hours maximum at 20°C. 


If the overcoating time of 24 hours is exceeded, the 545 Primer needs to be sanded with grit 150 prior to the application of the Hull-Gard ER.








U.S. PAINT - 09.10.1998











