6. AWLGRIP PAINTSYSTEM FOR ALUMINUM BELOW THE WATERLINE WITH HULL-GARD ER PRIMER





Steps�
Product name�
Mixing ratio in volume plus reducer�
Recoat time in hours/weeks at 20°C�
Application method�
Abrasive paper    


grit�
Coverage per liter mix.�
Total wet film thickness�
Total dry film thickness�
Remarks�
�
6.1.�
Surface preparation: 


Deoxidine�
N / A�
N / A�
N / A�
36�
N / A�
N / A�
N / A�
Don’t let Deoxidine dry on the surface, rinse thoroughly with water !�
�
�6.2.�
Hull-Gard ER Epoxy  Primer Cream


�
Kit - base + converter 73057


T0006	:  up to 10%�
In between coats :


min. : 3 hrs


max.: 8 wks�
Spray





          Roller�
N / A�
5,6 m² at 


75 micron�
150 micron�
75 


micron�
Roller application requires at least 2 coats.�
�
�6.3. �
Awlfair 


Light Weight


Fairing Compound�
Base	: 1              D8020


Conv.	: 1              D7007


�
min.:  24 hrs


max.: N/A


�
Knife





 Board�
40 - 80�
1m²/1mm�
N / A�
N / A �
Do not add thinner or reducer. Always sand in between coats !�
�
�6.4.�
Hull-Gard ER Epoxy Primer�
Kit - base + converter 73057


T0006 : up to 10%�
In between coats :


min. : 3 hrs


max.: N/A�
Spray





          Roller�
N / A �
5,6 m² at 


75 micron�
150 micron�
75 micron�
Roller application requires at least 2 coats.�
�
�6.5.�
Hull-Gard WB Epoxy Primer�
Kit - base + converter


Black 73152


White 73128


T0006 : up to 20%�
in between coats :


min. :  5 hrs


max.: 24 hrs�
Spray





             


          Roller�
 N / A�
3,2 m² at 200 micron�
400 micron�
300 micron�
Has to be applied in multiple coats.�
�
6.6.�
Anti-Fouling suitable for aluminum�
N / A�
N / A�
N / A�
N / A�
N / A�
N / A�
N / A�
Follow instructions manufacturer.�
�



For further information regarding surface treatment, application methods and product information see the description Awlgrip paintsystem n°6 for aluminum below the waterline + Awlgrip technical product datasheets.





Note: In case no fairing is required, after step 6.2. (application of Hull-Gard ER), one can proceed with step 6.5 (application of Hull-Gard WB).


U.S. PAINT - 09.10.1998











