7.AWLGRIP PAINTSYSTEM FOR NON-ANODIZED ALUMINUM MASTS





Steps�
Product name�
Mixing ratio in volume plus reducer�
Recoat time in hours at 20°C�
Application method�
Abrasive paper    


grit�
Coverage per liter mix.�
Total wet film thickness�
Total dry film thickness�
Remarks�
�
7.1.�
Surface preparation: Deoxidine / Scotchbrite�
N /A�
N / A�
N / A�
Scotchbrite�
N / A�
N / A�
N / A�
Don’t let Deoxidine dry on the surface, rinse thoroughly  with water!�
�
7.2.�
30-Y-94 Non-Sanding Anti-Corrosive Epoxy Primer�
Base         : 1          S9001


Converter : 1          S3001


T0006      : 50%�
min. : 3


max.: 6�
Spray�
N / A�
10m²�
75 micron�
20 micron�
Do not sand Mil Spec Primer 30-Y-94.�
�
7.3.�
545 Anti-Corrosive Epoxy Primer  


�
Base	: 1     Grey D1001


Conv.	: 1             D3001


T0006	:  up to 25%�
In between coats :


min.  :  2


max. : 24�
   Spray


�
80 - 120�
5 m² at 


60 micron�
175-250


micron


�
50-75 


micron�
May require multiple applications. 50 micron minimum has to remain after sanding!�
�
�7.4. �
Awlfair 


Light Weight


Fairing Compound�
Base	: 1              D8020


Conv.	: 1              D7007


�
min. : 24


max.: N/A�
Knife





 Board�
40 - 80�
1m²/1mm�
N / A�
N / A �
Do not add thinner or reducer. Always sand in between coats !�
�
7.5.


�
545 Epoxy Primer �
Base 	: 1   White  D8001


    or	  1   Gray   D1001


Conv.	: 1              D3001


T0006	:  up to 25%�
In between coats :


min.:   2


max.: 24


 �
Spray�
220-400�
5 m²�
175-250 micron�
50-75


micron�
In case more coats are required, allow a curing time of min. 8 hours in between the various coats.�
�
7.6.


�
Awlgrip Polyester


Urethane Topcoat�
Base	: 1    see colorcard


Conv.	: 1              G3010


T0001/T0003 : max. 25%�
In between coats :


30-45 min.�
Spray�
220-400�
6 m²�
150-200 micron�
50-75 


micron�
See guidelines for topcoat application.�
�
OR�
Awlgrip Polyester


Urethane Topcoat�
Base	: 2    see colorcard


Conv. 	: 1              H3002


T0031	: max. 25 %�
In between coats : overnight�
Brush �
220-400 or Scotch-Brite�
9 m²�
100-150 micron�
50-75 


micron�
Has to be applied in multiple coats�
�



For further information regarding surface treatment, application methods and product information see the description Awlgrip paintsystem n°7 for non-anodized aluminum masts + Awlgrip technical product datasheets.





Note: In case no fairing is required, after step 7.3 (application of 545 Primer), one can proceed with step 7.6. (application of Awlgrip Topcoat).


