	MAINTAINING AN AWLGRIP ® OR AWLCRAFT® 2000 TOPCOAT�PRIVATE ��





It is difficult for dirt, grime and grease to adhere to an AWLGRIP® or AWLCRAFT® 2000 Topcoat.  However, over time, a build up of dirt and grease and other contaminants can cause the finish to appear dull.





The mirror-like gloss can be easily maintained by following these simple rules:








DO:





1.	Wash the surface regularly with AWLWASH and water. Regular cleaning will avoid build up which can slowly attack the AWLGRIP® or AWLCRAFT® 2000 Topcoat, prematurely aging the coating.��Thoroughly rinse all surfaces with fresh water after washing to remove all detergent residue.��Wiping the surface dry with a chamois or soft cotton towel is recommended.








AWLGRIP® ONLY : 


�Solvents such as AWL-PREP® - T0008, AWL-PREP® PLUS T0115, toluene, lacquer thinner, MEK, acetone or kerosene may be used to soften or remove heavy build up of grease and grime, felt tip markings, or spray paint on the AWLGRIP® Topcoat. 





AWLCRAFT® 2000 ONLY :


Use only milder solvents to remove stubborn stains.  AWL-PREP® T0008, mineral spirits, xylene, kerosene, and diesel fuel are acceptable to use on AWLCRAFT® 2000.





FOR BOTH AWLGRIP® AND AWLCRAFT® 2000 :


Apply cleaning solvents with soft clean cloths. Wipe up solvent quickly. Do not allow solvent to dry on the surface or puddle and soak into the surface. Wash these areas with mild detergent and water to remove solvent residue.








3.	Always thoroughly rinse all surfaces with fresh water after cleaning with AWLWASH or solvents.


Latent solvent residue can attack the AWLGRIP® or AWLCRAFT® 2000 Topcoat, while detergent residue will attract dirt.








Use distilled white vinegar and hot water to remove stubborn salt stains.








5.	Use AWLCARE by hand to remove stubborn diesel soot stains.














�









DO NOT :





Do not wax. General : Wax build-up ages and yellows very rapidly, creating the need to maintain the wax and causing the topcoat to appear yellow. Wax build up also collects dirt, increasing maintenance.





AWLGRIP® Only : Waxing with a wax which contains no abrasives or cleaners will probably not hurt the surface, but at the same time offers no benefit.  Regular waxing will not increase the life of an AWLGRIP® Finish.  Wax can temporarily restore the gloss to small scuffs, scrapes, or scratches, sometimes allowing the postponement of repairs or repainting until a convenient time.





AWLCRAFT® 2000 ONLY : Waxing will help maintain the gloss on AWLCRAFT® 2000 Finishes, especially those which have been buffed or polished.  Remember-waxing leads to having to maintain the wax.  Do not wax areas unless they are dull or hazed.





2.	Do not use abrasives, scratch pads, or polishing compounds. Scratching the surface gives dirt a place to cling while wearing out the resin layer. Using abrasives of any kind will reduce the overall life of the finish and voids the AWLGRIP® Limited Warranty.








3.	Do not allow contact between AWLGRIP® or AWLCRAFT® 2000 Topcoat and teak cleaners. Most teak cleaners contain acids or caustic agents that stain and discolour the AWLGRIP® or AWLCRAFT® 2000 Topcoat.








4.	Do not use strong solvents (e.g., lacquer thinner, MEK, acetone) to clean AWLCRAFT® 2000, AWL-BRITE® or AWLSPAR® Varnish.








5.	Do not allow wet equipment (e.g., seat cushions, coils of line, sails, sailcovers, coolers) to trap and hold moisture against AWLGRIP® Topcoats. This condition can result in blistering or delamination of the AWLGRIP® or AWLCRAFT® 2000 Topcoat.








6.	Do not use acrylic teflon coatings over an AWLGRIP® or AWLCRAFT® 2000 Finish.  Use of these coatings void the AWLGRIP® Limited Warranty.





WINTER STORAGE


Do not "shrink wrap" or tightly bind AWLGRIP® or AWLCRAFT® 2000 Topcoat surfaces with plastic wrappings.





When tarping a boat for storage, the cover system should be ventilated allowing the system to "breathe". Covers and tarps, whether synthetic or of natural fiber, should not be pulled tight to surfaces painted with AWLGRIP® or AWLCRAFT® 2000 Topcoat. This condition can trap and hold moisture on the surface and may result in loss of gloss, blistering, or delamination of the topcoat.





Caution should also be used to ensure that the tarp does not chafe against the AWLGRIP® or AWLCRAFT® 2000 surface. Such chafing, especially when accompanied by airborne dirt, can abrade the surface and cause premature loss of gloss.





---------------------------------------


